[doc sps="1.8" acron="rconst" jtitle="Revista de la construcción" stitle="Revista de la Construcción" issn="0718-915X" eissn="0718-915X" pubname="Escuela de Construcción Civil, Pontificia Universidad Católica de Chile" license="http://creativecommons.org/licenses/by-nc/4.0" volid="21" issueno="2" dateiso="20220900" season="Sep./Dec" order="04" fpage="228" lpage="247" pagcount="20" doctopic="oa" language="en"]

https://doi.org/[doi]10.7764/RDLC.21.2.22[/doi]

[toctitle]RESEARCH ARTICLE[/toctitle]

[doctitle]Behaviour of sintered fly ash aggregates and steel fibers on reinforced concrete slabs subjected to punching[/doctitle]

[author role="nd"][fname]Ranjith[/fname] [surname]Babu B[/surname][xref ref-type="aff" rid="aff1"]1[/xref] [authorid authidtp="orcid"]https://orcid.org/0000-0002-4690-7834[/authorid][/author]

[author role="nd"][fname]Thenmozhi[/fname] [surname]R[/surname][xref ref-type="aff" rid="aff2"]2[/xref] [authorid authidtp="orcid"]https://orcid.org/0000-0002-5936-4402[/authorid][/author]

[normaff id="aff1" ncountry="Not normalized" norgname="Not normalized" icountry="IN"][label]1[/label]Department of Civil Engineering, [orgname]PSNA College of Engineering and Technology[/orgname], Dindigul, [city]Tamil Nadu [/city]([country]India[/country]), [email]ranjithbabucivil@psnacet.edu.in[/email][/normaff]

[normaff id="aff2" ncountry="Not normalized" norgname="Not normalized" icountry="IN"][label][sup]2[/sup][/label]Department of Civil Engineering, [orgname]Government College of Technology[/orgname], Coimbatore, [city]Tamil Nadu [/city]([country]India[/country]), [email]drthenmozhi@gct.ac.in[/email][/normaff]

[corresp id="c1"]Correspondence: [email]ranjithbabucivil@psnacet.edu.in[/email][/corresp]

[xmlabstr language="en"]Abstract: In this study the optimum replacement percentage of sintered fly ash aggregates in M30 grade of concrete was identified based on 28 days cubical compressive strength value. The optimum replacement of Sintered Fly ash Aggregates (SFA) is 40 %. Before identifying the optimum replacement percentage, the SFAs were tested for suitability test such as crushing strength test, impact test and water absorption test. Further, the optimum 40 % SFAs in concrete is tested for punching shear on the Reinforced Concrete (RC) slabs for a dimension of 1000 mm x 1000 mm x 100 mm. In addition to know the effect of steel fibers in RC slabs subjected to punching. A hook ended steel fibers having an aspect ratio of 55, 80 and 100 is selected and varied by volume of concrete for the punching shear values on RC slabs. The RC slabs concrete contains aspect ratio of steel fibers 55 is varied for 0.25 %, 0.5 %, 0.75 % and 1 % for volume of concrete. In addition to that a constant volume of steel fiber 0.5 % is selected for the aspect ratios of 80 and 100 for the punching shear tests. The punching shear values for the RC slabs shows that partial replacement of SFAs and steel fibers in concrete enhances the punching shear strength. These experimental tested results are compared with finite element programming (ABAQUS) and international codes such as IS 456 and ACI 2011. The experimental punching shear results were higher when compared to international codes.[/xmlabstr]

[kwdgrp language="en"][sectitle]Keywords:[/sectitle] [kwd]Sintered fly ash aggregates[/kwd], [kwd]steel fibers[/kwd], [kwd]punching shear strength[/kwd], [kwd]ABAQUS[/kwd], [kwd]IS 456[/kwd], [kwd]ACI 2011[/kwd][/kwdgrp].

[hist]Received: [received dateiso="20210321"]21.03.2021[/received]; Accepted: [accepted dateiso="20220805"]05.08.2022[/accepted]; Published: 30.08.2022[/hist]

- [xmlbody][sec sec-type="intro"][sectitle]Introduction[/sectitle]

[p]Managing industrial waste materials is one of the most important environmental issues. Concrete Technology can recommend some ways for reuse some industrial wastes such as fly ash (FA), silica fume (SF), and ground granulated blast furnace slag (GGBS). For the past two decades, usage of such minerals as a cement replacement material has been practiced by most of the invigilators. The concrete contains the aggregate made from municipal incinerated waste and Lytag (Commercial product name for sintered fly ash aggregate), shows that the Lytag aggregates proven that it is a better suitable for natural aggregates ([xref  ref-type="bibr" rid="r41"]Wainwright & Robery, 1997[/xref]). The usage of sintered fly ash lightweight aggregates to produce concrete, needs to be more understanding on the properties of the aggregates and they also concluded that high volume of cementitious content leads to undesirable for the structural application. Addition of steel fiber reinforcement significantly increases the tensile strength of lightweight aggregate concrete. The higher tensile strength together with low elastic modulus believed to be effective in reducing shrinkage cracking ([xref  ref-type="bibr" rid="r24"]Kayali, Haque & Zhu, 1999[/xref]). [/p]

[p]The pulverized fly ash as may be used up to 30% of cement replacement. However, utilization of industrial waste dust materials such as FA and GGBS in manufacturing of artificial aggregates attracted the invigilators and researchers as an alternative way to use in large (Kearsley, Wainwright & Amtsbuchler, 2005; [xref  ref-type="bibr" rid="r14"]Gesoğlu, Güneyisi, Mahmood, Öz & Mermerdaş, K, 2012[/xref]; [xref  ref-type="bibr" rid="r10"]Cheeseman, Makinde, & Bethanis, 2005[/xref]). The sintered fly ash aggregate concretes had higher compressive strength and modulus of elasticity than cold bonded aggregates ([xref  ref-type="bibr" rid="r27"]Kockal, & Ozturan, 2011[/xref]). Concrete production using cold bonded and sintered fly ash aggregates, concluded the sintered fly ash aggregates had a better mechanical properties and higher durability factors (Güneyisi, E, Gesoğlu, M, Pürsünlü & Mermerdaş, 2013). The punching shear strength on reinforced concrete slabs using combined natural and clay aggregates, shows that the incorporation of rounded aggregates in concrete possess less punching angle compared to natural aggregate concrete and the study concluded that the round shape of aggregates provides higher restriction to punching ([xref  ref-type="bibr" rid="r42"]Youm, Kim, Moon, 2014[/xref] & [xref  ref-type="bibr" rid="r4"]Babu B, R, 2021[/xref]). [/p]

[p]The addition of pozzolanic materials like GGBS (Ground Granulated Blast Furnace Slag) increases the punching shear capacity of slabs by 21% in normal strength concrete ([xref  ref-type="bibr" rid="r33"]Nemani, Rao & Grandhe, 2016[/xref]). The incorporation of lightweight aggregates in concrete produces reduction in self-weight of the structure and does not show reduction in aggregate interlock contribution in the punching zone ([xref  ref-type="bibr" rid="r8"]Caratelli, Imperatore, Meda & Rinaldi 2016[/xref]). The partial replacement of natural coarse aggregates with recycled aggregates leads to reduction in stiffness, energy absorption and punching shear strength. The main reason for this was the replaced recycled aggregates were highly water absorption ([xref  ref-type="bibr" rid="r29"]Mahmoud, El tony, tony & Saeed, 2018[/xref]). Mix design for production of concrete using sintered fly ash aggregates for the structural application based on tensile characteristics and also good in durability studies ([xref  ref-type="bibr" rid="r32"]Nadesan, & Dinakar, 2017[/xref]).  [/p]

[p]The effect of sintered fly ash aggregates in concrete, they report that sintered fly ash aggregates improved the thickness and quality of ITZ (interfacial transition zone) with higher structural efficiency compared to normal concrete ([xref  ref-type="bibr" rid="r32"]Nadesan, & Dinakar, 2017[/xref]). Research on punching shear strength of two-way reinforced concrete slabs is important to evaluate the safety in structural systems ([xref  ref-type="bibr" rid="r40"]Tuğrul Erdem, R, 2021[/xref]).  The flat slabs are supported directly on columns, without any intersection of beams between the columns. It generally transfers a significantly high concentrated load that acting on a relatively small area on the slab. Thus, the slab to column connection was a high concentration of shear stress. This localized stresses on the slab leads on punching risk. This phenomenon occurs suddenly (brittle fracture), which is why it has to be considered with careful design of slabs supported on columns only (e.g., in parking garages, office and residential buildings, bridges, etc.), but also in case of slabs lying below columns (e.g., foundation slabs or footings) ([xref  ref-type="bibr" rid="r6"]Bartolac, Damjanović & Duvnjak, 2015[/xref]). [/p]

[p]The volume of fibers (Vf) significantly affects the workability of the concrete mixtures. The most suitable value of Vf was in-between 0.5% to 2.5% by Volume of concrete ([xref  ref-type="bibr" rid="r38"]Shah, Daniel, Ahmad, Arockiasamy, Balaguru, Ball & Zollo, (1993[/xref]). The increase in punching shear was due to the occurrence of steel fibers. It was primarily controlled by the volume fraction and aspect ratio of steel fibers ([xref  ref-type="bibr" rid="r17"]Harajli, Maalouf & Khatib,1995[/xref]). The addition of steel fibers in concrete is not only an effective way to improve its tensile stress, toughness and durability. The incorporation of steel fibers in slabs increases the ductility, load carrying capacity ([xref  ref-type="bibr" rid="r5"]Balendran, Zhou, Nadeem & Leung, 2002[/xref]). The thickness design for the slab was based on post cracking behavior and concrete compressive strength ([xref  ref-type="bibr" rid="r26"]Kearsley, Elsabé & Elsaigh, 2003[/xref]). The steel fiber was one of the most popular and widely used fibers in both research and practice ([xref  ref-type="bibr" rid="r30"]Mohammadi, Singh, & Kaushik, 2008[/xref]). The steel fibers in concrete reduces the average crack width of the slab, increase initial stiffness and concrete ductility ([xref  ref-type="bibr" rid="r34"]Nguyen-Minh, Rovňák, Tran-Quoc & Nguyenkim, 2011[/xref]). [/p]

[p]The study of sintered fly ash aggregates in concrete is mostly in the forms of producing lightweight concrete and the failures in structural elements needs to be understood before using in to construction industry. [xref  ref-type="bibr" rid="r11"]Divyah N, Thenmozhi, R & Neelamegam M, 2020[/xref] studied the lightweight concrete made with sintered fly ash aggregate subjected to cyclic loading. [xref  ref-type="bibr" rid="r35"]Patra SN, Patra RK, Mukharjee BB, & Jena S, 2021[/xref] studied the partial replacement of sintered fly ash aggregate with natural aggregate with mineral admixture as metakaolin. This study shows that 30% sintered fly ash aggregate and 10-15% metakaolin performs well and the structural evaluation of combined sintered fly ash aggregate and natural coarse aggregate studies are limited and this combination of aggregates are identified as a research gap.  [/p]

[p]In this present investigation the punching shear strength of the reinforced concrete slab is measured by identifying the optimum sintered fly ash aggregate in concrete and also by varying the volume of steel fibers in concrete with respect to the aspect ratio of steel fibers.[/p]

- [/sec][sec sec-type="materials|methods"][sectitle]Materials and methods[/sectitle]

[p]The materials used in this work were Ordinary Portland Cement 53 (OPC 53), Chemical admixture (Conplast 430 sulphonated naphthalene), drinking water, natural sand, natural coarse aggregate and sintered fly ash aggregate (SFA) of 12.5 mm sieve passing, deformed high grade steel bars of 10 mm diameter with yield strength of 500 MPa and Hook ended steel fibers of aspect ratio 55, 80 and 100. [xref  ref-type="table" rid="t1"]Table 1[/xref] showed the properties of the steel fibers. Tests for the properties of the sintered fly ash aggregates were performed in compliance with Indian standard (IS 2386, 2002). The aggregates of Sintered fly ash were procured from GBC India private limited, Gujarat. The physical and mechanical properties of coarse aggregates used in this experimental system are shown in [xref  ref-type="table" rid="t2"]Table 2[/xref].[/p]

[tabwrap id="t1"][label]Table 1[/label]. [caption]Characteristics of hook ended steel fibers. [/caption]

[graphic href="?art04"][/graphic][/tabwrap]

[tabwrap id="t2"][label]Table 2[/label]. [caption]Physical and mechanical properties of natural and sintered fly ash aggregates.[/caption]

[graphic href="?art04"][/graphic][/tabwrap]

[p]2.1. Suitability level of sintered fly ash aggregates (SFAs) in concrete[/p]

[p]To identify the better replacement level of SFAs in concrete. The SFAs were replaced (by weight) 20%, 40% and 60% in natural coarse aggregates. The mechanical properties of these mixes were designed for a grade of M30 (IS10262, 2009) and their properties were shown in [xref  ref-type="table" rid="t3"]Table 3[/xref]. Based on the higher compressive strength of the concrete mixtures. The 40 % replacement of SFA was further investigated for punching shear strength on reinforced concrete slabs on the basis of steel fibers by varying volume and aspect ratio of steel fibers.[/p]

[tabwrap id="t3"][label]Table 3[/label]. [caption]Mechanical properties of SFAC mixtures. [/caption]

[graphic href="?art04"][/graphic][/tabwrap]

[p]2.2. Mix proportions of sintered fly ash aggregate concrete (SFAC)[/p]

[p]Sintered Fly Ash Aggregates (SFAs) must be wetted in concrete before its application. If the SFAs is not moist, water from the paste will be absorbed, thereby losing its workability in fresh state and the effective water / cement ratio in the paste ([xref  ref-type="bibr" rid="r15"]Gomathi & Sivakumar, 2015[/xref]) SFAs were held in water for 24hrs in this study and spread for four hours on a plastic sheet in free air before being used as Saturated Surface dry conditions (SSD). The concrete mixes were constructed in this test program according to Indian standard (IS10262, 2009). Seven concrete mixtures were developed for a 75-100 mm slump. Both blends employed the same volume of water and cement. The water-cement ratio was 0.35. Hook finished 25 percent volume steel fibers, 50 percent, 75 percent, and 100 percent with an aspect ratio of 55 in the concrete mixes. Likewise, for an aspect ratio of 80 and 100, 50 percent volume of hook-ended steel fibers were used. The mix ids and its average concrete mechanical properties are shown in [xref  ref-type="table" rid="t4"]Table 4[/xref].[/p]

[tabwrap id="t4"][label]Table 4[/label]. [caption]Fresh and hardened properties of SFAC mixtures. [/caption]

[graphic href="?art04"][/graphic][/tabwrap]

[p]2.3. Preparation of RC slab specimens[/p]

[p]The slabs, supports, and loading system dimensions were the same in all of the test. The square plan dimensions of all the slabs were 1000 mm x 1000 mm and 100 mm thick. The slabs were casted by making a wooden ply wood as a formwork material. The slabs were provided with steel reinforcement at bottom, 10 bars of 10 mm diameter in both the spanning directions, with an effective concrete cover of 20 mm as shown in [xref  ref-type="fig" rid="f1"]Figure 1[/xref]. The steel bars were 900 mm long placed at 100 mm centre - centre distance. The slab specimens were cured with water after casting for 28 days. The slab specimens were coated with white paint, in order to ensure good identification of cracks during and after processing.[/p]

[figgrp id="f1"][graphic href="?art04"][/graphic]

[label]Figure 1[/label]. [caption]Experimental test setup and reinforcement detailing.[/caption][/figgrp]

[p]2.3.1. Loading arrangements, measurements and testing procedure[/p]

[p][xref  ref-type="fig" rid="f2"]Figure 2[/xref] shows the selected restrained form. Researchers ([xref  ref-type="bibr" rid="r37"]Sermet & Ozdemir 2016[/xref], [xref  ref-type="bibr" rid="r36"]Reis, Brito, correia & Aruda 2015[/xref]) have commonly used this form of restrained, and it reflects the general flat slab actions. The load cell recording the load and a plate of 150 mm diameter and 20 mm thickness were located from top to bottom of the hydraulic jack, respectively. Loading is carried out through the steel plate in the center of the slab. The Linear Variable Displacement Transducer (LVDT) was used for calculating slab deflection at mid-span. Measuring network of data loggers used to calculate loads and deflections. The load was applied up to 5 kN in increment. Deflections were reported via read out system during the study. The initiation and propagation of cracks were controlled at load intervals by visual inspection.[/p]

[figgrp id="f2"][graphic href="?art04"][/graphic]

[label]Figure 2[/label]. [caption]Loading arrangements for punching on a RC slab.[/caption][/figgrp]

- [/sec][sec sec-type="results|discussion"][sectitle]Experimental results and discussions[/sectitle]

[p]The load - deflection relationships for the tested slab specimens concrete having 40% of sintered fly ash aggregates and aspect ratio of steel fibers 55 were shown in [xref  ref-type="fig" rid="f3"]Figure 3[/xref]. From the load -deflection chart the ultimate load was nothing but punching shear strength of the slabs. The addition of steel fibers in concrete contains 40 % of sintered fly ash aggregates increases the punching shear values as 11.02 %, 10.23 %, 15.74 % and 28.34 %. As the fiber dosages increases the punching shear strength increases linearly. In addition to that the presence of 40 % sintered fly ash aggregates made a better interlocking with the steel fibers and 60 % of natural aggregates.[/p]

[figgrp id="f3"][graphic href="?art04"][/graphic]

[label]Figure 3[/label]. [caption]Load - deflection values for concrete contains steel fibers of aspect ratio 55.[/caption][/figgrp]

[p]The minimum volume of steel fibers added in concrete to increase the punching shear strength was 0.5 % in volume of concrete. To study this phenomenon with respect to aspect ratio of steel fibers. The 0.5 % volume of fibers were varied in steel fibers aspect ratio by 55, 80 and 100. The varied concrete slab specimens load - deflection values were shown in [xref  ref-type="fig" rid="f4"]Figure 4[/xref]. Compared to concrete slabs without fibers the aspect ratio 80 and 100 increases the punching shear strength by 51.18 % and 10.23 %.  The concrete slab specimens carrying steel fibers of aspect ratio 55 and 100 got the same increased punching shear strength. This was due to larger length of the steel fibers for an aspect ratio of 100.[/p]

[figgrp id="f4"][graphic href="?art04"][/graphic]

[label]Figure 4[/label]. [caption]Load - deflection values for concrete contains steel fibers of aspect ratio 80 and 100.[/caption][/figgrp]

  - [p]Energy absorption capacity[/p]

[p]Energy absorption is known as one of the toughness parameter measurements. In the case of concrete structures, the area under load-deflection curve for the slab specimens can be defined. [xref  ref-type="fig" rid="f5"]Figure 5[/xref] displayed the measured energy-absorption values for each concrete mix.[/p]

[figgrp id="f5"][graphic href="?art04"][/graphic]

[label]Figure 5[/label]. [caption]Energy absorption capacity of concrete mixtures.[/caption][/figgrp]

[p]For each concrete mixture, the energy absorption potential has been increased as the amount of steel fibers only increases to 0.5 per cent. This amount of 0.5 per cent steel fibers was further varied with aspect ratio like 80 and 100. The normal concrete contains 40 percent of sintered fly ash aggregates from these energy absorption values and 0.5 percent of steel fibers having an aspect ratio of 80 were more resistant to punching shear force. The aspect ratio 100 provided less energy absorption compared with an aspect ratio of 55 and 80. It was concluded that 40 per cent of sintered fly ash aggregates need proper selection on the volume of steel fibers and the aspect ratio of steel fibers to increase the punching shear strength of concrete.[/p]

  - [p]Cracking and failure pattern[/p]

[p][xref  ref-type="fig" rid="f6"]Figure 6[/xref] displays the final crack patterns on all tested specimens. The cracks on the bottom sides are found to have been radial, mainly running between the loading point and the corners. A circular punching crack covering the load of patches occurred on the top surfaces and this was repeated with an expanded region on the bottom, clearly identifying the truncated cone. Similar pattern was reported by ([xref  ref-type="bibr" rid="r28"]Kuang & Morley, 1993[/xref]) on the lightweight aggregate concrete having hook ended steel fibers. The failure modes of the slab were in the form of flexural failure when the concrete mixtures contain steel fibers. The addition of fibers can be taken as one such the way to improve the RC slabs against punching shear failure. This similar type of punching shear failure was attained where slab contains lightweight fiber reinforced concrete with ashes from municipal solid wastes ([xref  ref-type="bibr" rid="r8"]Caratelli, Imperatore, Meda & Rinaldi, 2016[/xref]).[/p]

[figgrp id="f6"][graphic href="?art04"][/graphic]

[label]Figure 6[/label]. [caption]Failure patterns of slabs for different mixtures[/caption][/figgrp]

  - [p]ABAQUS modeling and results[/p]

[p]The Finite element analysis (ABAQUS) can be used as an assessment tool and it can provide insights into punching shear failure and crack formation. The slab model has been developed in the finite element-based software ABAQUS. This programme is capable of stimulating a non-linearity material like concrete and steel material and it has been widely used for reinforced concrete structure’s subjected to repeated loads and static loading. In order to simulate the tested slab, a full-scale model was modelled using the ABAQUS Manual (2014). The loading disc was applied by a downward displacement experienced from experimental value, to stimulate the real experimental behaviour. The modelled Reinforced concrete slab & loading disc were shown in [xref  ref-type="fig" rid="f7"]Figure 7[/xref].[/p]

[figgrp id="f7"][graphic href="?art04"][/graphic]

[label]Figure 7[/label]. [caption]Geometry of the RC slab.[/caption][/figgrp]

[p]The concrete material properties used in the present analyses are: The initial tangent modulus, secant modulus, Poisson’s ratio, compressive strength and split tensile strength for the selected concrete mixtures. The Poisson’s ratio has to be taken as a constant value such as ‘0.2’ for the cracked concrete. The dilation angle (ψ) 50, the shape factor (Kc) 0.667, the stress ratio (fb0/fc0) 1.16, Viscosity parameter (μ) 0.01 and the eccentricity (ϵ) 0.1. The f’c was calculated based on compressive strength of the cubes as taken as f’c =0.8 times fck. The concrete compressive behaviour was derived with the help of Hongnestad type parabola. The typical Hongnestad type parabolic curve is shown in the [xref  ref-type="fig" rid="f8"]Figure 8[/xref]. This parabolic curve was based on initial modulus of elasticity (Eo) = 5500f'c  and the Secant Elastic modulus (Esec) = 5000f'c. The linear branch ends at the 0.4 times the maximum stress value. The peak load corresponding strain ϵo=2f'cEsec.[/p]

[figgrp id="f8"][graphic href="?art04"][/graphic]

[label]Figure 8[/label]. [caption]Uniaxial compression stress - strain relationship for concrete. ([xref  ref-type="bibr" rid="r12"]Genikomsou & Polak, 2015[/xref])[/caption][/figgrp]

[p]The tensional behaviour was derived by making a tension stiffening curve with the help of fracture energy (Gf) values based on cylindrical strength of the concrete mixtures (f’c) as shown in Equation 1. This equation was based on the CEB-FIB model code of version 2010.Where, characteristic length (lc) was adopted as 20 mm. and f’t was split tensile strength of the concrete mixtures.[/p]

[figgrp id="ch1"][graphic href="?art04"][/graphic][/figgrp]

[p]The tension stiffening curve was based on the bilinear stiffening response. The bilinear response of concrete and development of the curve model was shown [xref  ref-type="fig" rid="f9"]Figure 9[/xref].[/p]

[figgrp id="f9"][graphic href="?art04"][/graphic]

[label]Figure 9[/label]. [caption]Development of tensile stress - strain model for concrete. ([xref  ref-type="bibr" rid="r12"]Genikomsou & Polak, 2015[/xref]).[/caption][/figgrp]

[p]The uniaxial stress - strain relationship for steel reinforcement and steel disc was modelled with an elastic property of young’s modulus and Poisson’s ratio as 20000 MPa and 0.3 respectively. The plastic properties used for reinforced bar was shown in [xref  ref-type="table" rid="t5"]Table 5[/xref]. The plastic properties were based on the tested results with a bilinear strain hardening yield stress - Plastic strain curve. An average mesh size of 20 mm was used to obtain the load - deflection curve. C3D8R has been used for concrete mesh, C3D8R has been used for steel bar mesh and C3D8R has been used for steel loading disc mesh.[/p]

[tabwrap id="t5"][label]Table 5[/label]. [caption]Plastic properties used for reinforced bar. [/caption]

[graphic href="?art04"][/graphic][/tabwrap]

[p]3.3.1 Finite element analysis results and discussion[/p]

[p]The finite element analysis results give a proper failure mode of the RC slab specimens which will help how the load dissipated to the specimens and the failure behaviour. In general, the loading disc punches the RC slabs at the centre and propagates the punching failure. The punching failure in RC slabs occur when the applied shear force exceeds the concrete mixture shear force. A general failure pattern of RC slabs contains sintered fly ash aggregates and steel fibers was simulated by the ABAQUS was shown in [xref  ref-type="fig" rid="f10"]Figure 10[/xref].[/p]

[figgrp id="f10"][graphic href="?art04"][/graphic]

[label]Figure 10[/label]. [caption]Failure stage of the RC slabs subjected to punching shear force.[/caption][/figgrp]

[p]The [xref  ref-type="fig" rid="f10"]Figure 10[/xref] shows the failure of RC slabs subjected to punching, from this failure we can clearly observe that once a high concentrated force was applied on the top of the slab, the support will be standing alone. The punched slab area will fall down. The red shaded area was the dissipation of shear stress to the supports and the blue shaded area were the slab disjointed from the slab. The [xref  ref-type="fig" rid="f11"]Figure 11[/xref] shows the comparison of load - deflection curve for the RC slabs subjected to punching for both experimental and ABAQUS. The ratio between experimental values and ABAQUS values shown in the [xref  ref-type="table" rid="t6"]Table 6[/xref]. For all the slab specimens punching shear strength values were correctly predicted by ABAQUS.[/p]

[figgrp id="ch2"][graphic href="?art04"][/graphic]
[/figgrp][figgrp id="ch3"][graphic href="?art04"][/graphic][/figgrp]
[figgrp id="f11"][graphic href="?art04"][/graphic]

[label]Figure 11[/label]. [caption]Load - deflection curves.[/caption][/figgrp]

[p]The PEMAG of the bottom RC slabs were shown in the [xref  ref-type="fig" rid="f12"]Figure 12[/xref]. The PEMAG shows the failure strains of the RC slabs for all the slabs. It clearly shows that the concrete mixture contains 40 % of sintered fly ash aggregates and steel fibers of volume as 0.25 %, 0.5 % and 0.75 % for the aspect ratio of 55 shows the greater absorption of energy and failure cone at the centre. For the aspect ratio 80 also the same behaviour. For the RC slabs SFA40 concrete contains 40 % sintered fly ash aggregates, the RC slab SFA40100 concrete contains 40 % Sintered fly ash aggregates and the volume of 1.0% of steel fibers for an aspect ratio 55. SFA4050100 concrete contains 40 % sintered fly ash aggregates and 0.5 % of volume steel fibers for an aspect ratio 100 shows the same behaviour. The addition of fibers in concrete slabs was highly depended on the aspect ratio and the volume. The PEMAG gives the failure patterns exactly compared to experimental failure patterns ([xref  ref-type="bibr" rid="r13"]Genikomsou AS, & Polak MA, 2016[/xref]). On comparing the PEMAG [xref  ref-type="fig" rid="f12"]Figure 12[/xref] with experimental failures. The RC slabs fails at centre of the slab and thus it leads to pure punching.[/p]

[figgrp id="ch4"][graphic href="?art04"][/graphic]
[/figgrp][figgrp id="f12"][graphic href="?art04"][/graphic]

[label]Figure 12[/label]. [caption]Failure patterns of RC slabs in ABAQUS for different mixtures[/caption][/figgrp]

  - [p]International design codes and its provisions [/p]

[p]Codes of practices of several countries like Indian standard and American concrete institute code present a generalized formula, where the punching load is a product of design nominal shear strength and the area of a chosen critical failure surface. Depending on the code of a country, the critical section for checking punching shear in slabs is taken at 0.5 to 2 times the effective depth from the edge of the load or the reaction.[/p]

[p]Generally, the punching shear strength values specified in different codes vary with concrete compressive strength or cylindrical strength. In Indian code IS 456; the punching shear strength is expressed as proportional to √ (fck). the square root formulae available in the Indian code is adopted from the ACI 318 Code.  This international design codes from equations (1) & (2) were used to predict ultimate punching load for the tested slabs. The results are shown in [xref  ref-type="table" rid="t6"]Table 6[/xref].[/p]

[p]3.4.1 American Concrete Institute Code ACI-318 - 2011[/p]

[p]The ultimate Punching shear is the smallest of[/p]

[p]Pu=0.17(1+2/β) √(fcy) λ(bo x d) 		(1a)[/p]

[p]Pu=0.083((αs x d)/bo ) √(fcy) λ(bo x d)         (1b)[/p]

[p]Pu=0.33√(fcy) λ(bo x d)   			(1c)[/p]

[p]where,[/p]

[list listtype="bullet"][li]Pu = Ultimate Punching shear strength, kN.[/li]

[li]fcy = Cylindrical compressive strength, MPa (Converting by 0.8 times cubical strength)[/li]

[li]bo = Perimeter of critical section (mm), π (Column Diameter + Effective depth); 723 mm[/li]

[li]d = Effective depth of the slab (mm)[/li]

[li]β = The ratio of long side to short side of the column of the concentrated load.[/li]

[li]λ = 1.0 for Normal strength concrete.[/li]

[li]αs = Coefficient depends on the position of the column.[/li]

[li]αs= 40 for inner column, 30 for edge column, 20 for corner column.[/li][/list]

[p]3.4.2 Indian Standard Code IS456-2000[/p]

[p]As per IS 456: 2000, the expression for calculating the punching shear strength Pu by considering partial safety factor for the material as unity is given by[/p]

[p]Pu= ks x τuc x bo x d   				 (2a)[/p]

[p]Where,[/p]

[list listtype="bullet"][li]Pu = Ultimate Punching shear strength, kN[/li]

[li]ks = (0.5+ β) < 1[/li]

[li]τuc = Shear strength in concrete, MPa[/li]

[li]τuc = 0.25√ (fck)[/li]

[li]fck= Characteristic compressive strength of concrete, MPa[/li]

[li]bo = Perimeter of critical section (mm), π (Column Diameter + Effective depth); 723 mm[/li]

[li]d = Effective depth of the slab (mm).[/li][/list]

[p]The comparison between ultimate punching load and predicted from code equations presented in [xref  ref-type="table" rid="t6"]Table 6[/xref].[/p]

[tabwrap id="t6"][label]Table 6[/label]. [caption]Comparison ultimate punching load experimental, international codes and ABAQUS. [/caption]

[graphic href="?art04"][/graphic][/tabwrap]

[p]The code results were appropriate if we know the cubical compressive strength of the concrete mixtures. In our concrete mixes, only the direct parameter which we can know was the compressive strength values. To know the real behavior of the RC slabs subjected to punching, an experimental test has to be carried out in the laboratory by making a small-scale specimen, or by using the ABAQUS modelling. Finally, the code book values are only a theoretical value. It will not give the failure modes. It seems that the addition of sintered fly ash aggregates and steel fibers increases the punching shear strength value.[/p]

  - [p]Theoretical evaluation[/p]

[p]The nominal failure moment (Mn) for the RC slabs contains 40 % SFA and different volume with varying aspect ratios of steel fibers was obtained using a theoretical model of their cross -section.    [/p]

[p]   [/p]

[p]3.5.1 Assumptions in theoretical analysis[/p]

[p]The current established model was based on the rectangular stress block. The recommended assumptions can be listed as follows. The adopted stress block was shown in [xref  ref-type="fig" rid="f13"]Figure 13[/xref]. ([xref  ref-type="bibr" rid="r7"]Basha, Fayed & Mansour, 2020[/xref])[/p]

- [list listtype="order"][li]Plane sections remains same before bending and after bending.[/li]

- [li]The tension force developed in the concrete was ignored.[/li]

- [li]An equivalent rectangular stress block was adopted to calculate the compressive force in concrete.[/li]

- [li]The partial safety factor for concrete and steel as taken by 1.5 and 1.15.[/li][/list]

[figgrp id="f13"][graphic href="?art04"][/graphic]

[label]Figure 13[/label]. [caption]Analytical model for RC slab.[/caption][/figgrp]

[p]The failure moment of the RC slab section was calculated based on the following equation. The calculate failure punching shear strength and comparison with the experimental values were shown in the [xref  ref-type="table" rid="t7"]Table 7[/xref]. The failure punching shear calculation was based on the basic structural analysis. [/p]

[figgrp id="ch5"][graphic href="?art04"][/graphic][/figgrp]

[figgrp id="ch6"][graphic href="?art04"][/graphic][/figgrp]

[p]where, [/p]

[list listtype="bullet"][li]Mn = Nominal failure moment value[/li]

[li]Ts = Tensile strength of the steel Bars[/li]

[li]d = Effective depth of the RC slab = 80 mm[/li]

[li]a = Height of the rectangular compressive stress block [/li]

[li]c = Location of the neutral axis[/li]

[li]Ast = Area of the steel reinforcement[/li]

[li]fy = Yield strength of the steel bars[/li]

[li]fcu = Cubical compressive strength of the concrete[/li]

[li]b = width of the slab, taken as 1 m[/li][/list]

[tabwrap id="t7"][label]Table 7[/label]. [caption]Punching shear strength values based on theoretical model. [/caption]

[graphic href="?art04"][/graphic][/tabwrap]

[p]The punching shear values computed based on the theoretical model shows a reasonable ratio when compared to the experimental punching shear strength value. It varies from 0.68 - 1.05.[/p]

- [/sec][sec sec-type="conclusions"][sectitle]Conclusion[/sectitle]

[p]The study of sintered fly ash aggregates and steel fibers in normal concrete gives the following conclusions,[/p]

- [list listtype="order"][li]The water absorption of sintered fly ash aggregates was 16.8 % after 24 hrs. While mixing with the concrete it absorbs more water. To avoid this excess absorption, aggregates were used under surface saturated condition;[/li]

- [li]The tested impact and crushing strength values of sintered fly ash aggregates meets the standards of natural aggregates;[/li]

- [li]The partial replacement (by weight) of sintered fly ash aggregates increases the slump values by 1.4, 1.75 and 2.05 times compared to normal concrete slump value;[/li]

- [li]The partial replacement (by weight) of sintered fly ash aggregates increases the compressive strength values by 7.16 %, 27.50 % and 11.30 % compared to normal concrete compressive strength values;[/li]

- [li]The partial replacement (by weight) of sintered fly ash aggregates increases the split tensile strength values by 4.08%, 45.72 % and 14.86 % compared to normal concrete compressive strength values;[/li]

- [li]The replacement of 40 % (by weight) sintered fly ash aggregates in normal concrete increases compressive strength and split tensile strength of the concrete mixtures;[/li]

- [li]The addition of steel fibers in concrete contains 40 % sintered fly ash aggregates and 60 % natural aggregates decreases the slump values linearly as the fiber dosage increases;[/li]

- [li]The incorporation of steel fibers in the concrete mixtures decreases the compressive strength. and split tensile values increase for 0.5 % volume of steel fibers for aspect ratio 55. The short fibers increase the tensile strength;[/li]

- [li]The punching shear strength and energy absorption were high when compared to remaining concrete mixtures. Particularly, the 0.5% steel fibers of aspect ratio 80 performed well;[/li]

- [li]The finite element software ABAQUS gives the same experimental performance for all the concrete mixtures. This can be useful to know how the crack propagates in the RC slabs;[/li]

- [li]The PEMAG represents the failure of the RC slabs in terms of plastic strains;[/li]

- [li]The experimental punching shear strength values were low when compared to IS 456 and ACI 318 predictions;[/li]

- [li]The theoretical model for the RC slabs subjected to punching shear strength was evaluated properly making an assumption. The stress block considered was rectangular shape.[/li][/list][/sec][/xmlbody]

[ack][sectitle]Author contributions: [/sectitle] Each author contributed for the design and implementation of the research, for the analysis of the results and to write this manuscript. [/ack]

[ack][sectitle]Funding: [/sectitle] None [/ack]

[ack][sectitle]Acknowledgments:[/sectitle] The author received no financial support for this research, authorship, and/or publication of this article [/ack].

[ack][sectitle]Conflicts of interest: [/sectitle] The authors declare that they have no conflict of interest [/ack].

[refs][sectitle]References[/sectitle]

[ref id="r1" reftype="book"][authors role="nd"][cauthor]ABAQUS Theory Manual (6.14)[/cauthor][/authors], [date dateiso="20140000" specyear="2014"]2014[/date]. [source]Dassault Systems[/source], [publoc]Providence, RI, USA[/publoc].[/ref]

[ref id="r2" reftype="book"][authors role="nd"][cauthor]ACI 318-11[/cauthor][/authors], [source]Building code Requirements for structural concrete and commentary[/source], [date dateiso="20110000" specyear="2011"]2011[/date].[/ref]

[ref id="r3" reftype=“journal"][authors role="nd"][pauthor][surname]Alwash[/surname], [fname]N. A.[/fname][/pauthor], & [pauthor][surname]Habbeb[/surname], [fname]G[/fname][/pauthor][/authors]. ([date dateiso="20170000" specyear="2017"]2017[/date]). [arttitle]Experimental and Numerical Investigation on The Punching Behavior of High Strength RC Flat Slab Under Repeated Load[/arttitle]. [source]J. Babylon Univ. Eng. Sci[/source]., [volid]25[/volid]([issueno]2[/issueno]), [pages]479-494[/pages].[/ref]

[ref id="r4" reftype=“journal"][authors role="nd"][pauthor][surname]Babu B[/surname], [fname]R[/fname][/pauthor][/authors]. ([date dateiso="20210000" specyear="2021"]2021[/date]). [arttitle]Experimental and numerical studies on punching shear strength of concrete slabs containing sintered fly ash aggregates[/arttitle]. [source]Revista de la construcción[/source], [volid]20[/volid]([issueno]1[/issueno]), [pages]15-25[/pages].[/ref]

[ref id="r5" reftype=“journal"][authors role="nd"][pauthor][surname]Balendran[/surname], [fname]R. V.[/fname][/pauthor], [pauthor][surname]Zhou[/surname], [fname]F. P.[/fname][/pauthor], [pauthor][surname]Nadeem[/surname], [fname]A.[/fname][/pauthor], & [pauthor][surname]Leung[/surname], [fname]A. Y. T[/fname][/pauthor][/authors]. ([date dateiso="20020000" specyear="2002"]2002[/date]). [arttitle]Influence of steel fibres on strength and ductility of normal and lightweight high strength concrete[/arttitle]. [source]Building and environment[/source], [volid]37[/volid]([issueno]12[/issueno]), [pages]1361-1367[/pages].[/ref]

[ref id="r6" reftype=“journal"][authors role="nd"][pauthor][surname]Bartolac[/surname], [fname]M.[/fname][/pauthor], [pauthor][surname]Damjanović[/surname], [fname]D.[/fname][/pauthor], & [pauthor][surname]Duvnjak[/surname], [fname]I[/fname][/pauthor][/authors]. ([date dateiso="20150000" specyear="2015"]2015[/date]). [arttitle]Punching strength of flat slabs with and without shear reinforcement[/arttitle]. [source]Građevinar[/source], [volid]67[/volid]([issueno]08[/issueno].), [pages]771-786[/pages].[/ref]

[ref id="r7" reftype=“journal"][authors role="nd"][pauthor][surname]Basha[/surname], [fname]A.[/fname][/pauthor], [pauthor][surname]Fayed[/surname], [fname]S.[/fname][/pauthor], & [pauthor][surname]Mansour[/surname], [fname]W[/fname][/pauthor][/authors]. ([date dateiso="20200000" specyear="2020"]2020[/date]). [arttitle]Flexural strengthening of RC one-way solid slab with Strain Hardening Cementitious Composites (SHCC)[/arttitle]. [source]Advances in concrete construction[/source], [volid]9[/volid]([issueno]5[/issueno]), [pages]511-527[/pages].[/ref]

[ref id="r8" reftype=“journal"][authors role="nd"][pauthor][surname]Caratelli[/surname], [fname]A.[/fname][/pauthor], [pauthor][surname]Imperatore[/surname], [fname]S.[/fname][/pauthor], [pauthor][surname]Meda[/surname], [fname]A.[/fname][/pauthor], & [pauthor][surname]Rinaldi[/surname], [fname]Z[/fname][/pauthor][/authors]. ([date dateiso="20160000" specyear="2016"]2016[/date]). [arttitle]Punching shear behavior of lightweight fiber reinforced concrete slabs[/arttitle]. [source]Composites Part B: Engineering[/source], [volid]99[/volid], [pages]257-265[/pages].[/ref]

[ref id="r9" reftype="book"][authors role="nd"][cauthor]CEB[/cauthor][/authors] - [source]FIB model code for concrete structures 2010[/source]. [pubname]Ernst & sohn[/pubname]; [date dateiso="20130000" specyear="2013"]2013[/date].[/ref]

[ref id="r10" reftype=“journal"][authors role="nd"][pauthor][surname]Cheeseman[/surname], [fname]C. R.[/fname][/pauthor], [pauthor][surname]Makinde[/surname], [fname]A.[/fname][/pauthor], & [pauthor][surname]Bethanis[/surname], [fname]S[/fname][/pauthor][/authors]. ([date dateiso="20050000" specyear="2005"]2005[/date]). [arttitle]Properties of lightweight aggregate produced by rapid sintering of incinerator bottom ash[/arttitle]. [source]Resources, Conservation and Recycling[/source], [volid]43[/volid]([issueno]2[/issueno]), [pages]147-162[/pages].[/ref]

[ref id="r11" reftype=“journal"][authors role="nd"][pauthor][surname]Divyah[/surname], [fname]N.[/fname][/pauthor], [pauthor][surname]Thenmozhi[/surname], [fname]R.[/fname][/pauthor], & [pauthor][surname]Neelamegam[/surname], [fname]M[/fname][/pauthor][/authors]. ([date dateiso="20200000" specyear="2020"]2020[/date]). [arttitle]Experimental and Numerical Analysis of Battened Built-up Lightweight Concrete Encased composite columns subjected to axial cyclic loading[/arttitle]. [source]Latin American Journal of Solids and Structures[/source], [volid]17[/volid].[/ref]

[ref id="r12" reftype=“journal"][authors role="nd"][pauthor][surname]Genikomsou[/surname], [fname]A. S.[/fname][/pauthor], & [pauthor][surname]Polak[/surname], [fname]M. A[/fname][/pauthor][/authors]. ([date dateiso="20150000" specyear="2015"]2015[/date]). [arttitle]Finite element analysis of punching shear of concrete slabs using damaged plasticity model in ABAQUS[/arttitle]. [source]Engineering Structures[/source], [volid]98[/volid], [pages]38-48[/pages].[/ref]

[ref id="r13" reftype=“journal"][authors role="nd"][pauthor][surname]Genikomsou[/surname], [fname]A. S.[/fname][/pauthor], & [pauthor][surname]Polak[/surname], [fname]M. A[/fname][/pauthor][/authors]. ([date dateiso="20160000" specyear="2016"]2016[/date]). [arttitle]Finite-element analysis of reinforced concrete slabs with punching shear reinforcement[/arttitle]. [source]Journal of Structural Engineering[/source], [volid]142[/volid]([issueno]12[/issueno]), [pages]04016129[/pages].[/ref]

[ref id="r14" reftype=“journal"][authors role="nd"][pauthor][surname]Gesoğlu[/surname], [fname]M.[/fname][/pauthor], [pauthor][surname]Güneyisi[/surname], [fname]E.[/fname][/pauthor], [pauthor][surname]Mahmood[/surname], [fname]S. F.[/fname][/pauthor], [pauthor][surname]Öz[/surname], [fname]H. Ö.[/fname][/pauthor], & [pauthor][surname]Mermerdaş[/surname], [fname]K[/fname][/pauthor][/authors]. ([date dateiso="20120000" specyear="2012"]2012[/date]). [arttitle]Recycling ground granulated blast furnace slag as cold bonded artificial aggregate partially used in self-compacting concrete[/arttitle]. [source]Journal of hazardous materials[/source], [volid]235[/volid], [pages]352-358[/pages].[/ref]

[ref id="r15" reftype=“journal"][authors role="nd"][pauthor][surname]Gomathi[/surname], [fname]P.[/fname][/pauthor], & [pauthor][surname]Sivakumar[/surname], [fname]A[/fname][/pauthor][/authors]. ([date dateiso="20150000" specyear="2015"]2015[/date]). [arttitle]Accelerated curing effects on the mechanical performance of cold bonded and sintered fly ash aggregate concrete[/arttitle]. [source]Construction and building Materials[/source], [volid]77[/volid], [pages]276-287[/pages].[/ref]

[ref id="r16" reftype=“journal"][authors role="nd"][pauthor][surname]Güneyisi[/surname], [fname]E.[/fname][/pauthor], [pauthor][surname]Gesoğlu[/surname], [fname]M.[/fname][/pauthor], [pauthor][surname]Pürsünlü[/surname], [fname]Ö.[/fname][/pauthor], & [pauthor][surname]Mermerdaş[/surname], [fname]K[/fname][/pauthor][/authors]. ([date dateiso="20130000" specyear="2013"]2013[/date]). [arttitle]Durability aspect of concretes composed of cold bonded and sintered fly ash lightweight aggregates[/arttitle]. [source]Composites Part B: Engineering[/source], [volid]53[/volid], [pages]258-266[/pages].[/ref]

[ref id="r17" reftype=“journal"][authors role="nd"][pauthor][surname]Harajli[/surname], [fname]M. H.[/fname][/pauthor], [pauthor][surname]Maalouf[/surname], [fname]D.[/fname][/pauthor], & [pauthor][surname]Khatib[/surname], [fname]H[/fname][/pauthor][/authors]. ([date dateiso="19950000" specyear="1995"]1995[/date]). [arttitle]Effect of fibers on the punching shear strength of slab-column connections[/arttitle]. [source]Cement and Concrete Composites[/source], [volid]17[/volid]([issueno]2[/issueno]), [pages]161-170[/pages].[/ref]

[ref id="r18" reftype="book"][authors role="nd"][cauthor]IS 10262[/cauthor][/authors]: [date dateiso="20090000" specyear="2009"]2009[/date], [source]Concrete Mix Proportioning - Guidelines[/source], [pubname]Bureau of Indian Standards[/pubname]. [publoc]New Delhi[/publoc]-[pages]12[/pages].[/ref]

[ref id="r19" reftype="book"][authors role="nd"][cauthor]IS 2386[/cauthor][/authors], [source]Methods of test for aggregates for concrete[/source], [pubname]Bureau of Indian Standards[/pubname]. [publoc]New Delhi[/publoc], [date dateiso="19630000" specyear="1963"]1963 [/date]&#091;[moreinfo]Reaffirmed in 2002[/moreinfo]&#093;.[/ref]

[ref id="r20" reftype="book"][authors role="nd"][cauthor]IS 456-2000[/cauthor][/authors], [source]Indian standard code of practice for plain and reinforced concrete[/source], [date dateiso="20000000" specyear="2000"]2000[/date].[/ref]

[ref id="r21" reftype="book"][authors role="nd"][cauthor]IS: 2386[/cauthor][/authors], [source]Indian Standard Specification, Methods of Test for Aggregates for Concrete: Part 3, Specific Gravity, Density, Voids, Absorption and Bulking[/source], [pubname]Bureau of Indian Standards[/pubname], [publoc]New Delhi[/publoc], [date dateiso="19630000" specyear="1963"]1963 [/date]&#091;[moreinfo]Reaffirmed in 2002[/moreinfo]&#093;.[/ref]

[ref id="r22" reftype="book"][authors role="nd"][cauthor]IS: 2386[/cauthor][/authors], [source]Indian Standard Specification, Methods of Test for Aggregates for Concrete: Part 4[/source], [pubname]Mechanical Properties Bureau of Indian Standards[/pubname], [publoc]New Delhi[/publoc], [date dateiso="19630000" specyear="1963"]1963 [/date]&#091;[moreinfo]Reaffirmed in 2002[/moreinfo]&#093;.[/ref]

[ref id="r23" reftype="book"][authors role="nd"][cauthor]IS: 2386[/cauthor][/authors], [source]Indian Standard Specification, Methods of Test for Aggregates for Concrete: Part 1 Particle Size and Shape[/source], [pubname]Bureau of Indian Standards[/pubname], [publoc]New Delhi[/publoc], [date dateiso="19630000" specyear="1963"]1963 [/date]&#091;[moreinfo]Reaffirmed in 2002[/moreinfo]&#093;.[/ref]

[ref id="r24" reftype=“journal"][authors role="nd"][pauthor][surname]Kayali[/surname], [fname]O.[/fname][/pauthor], [pauthor][surname]Haque[/surname], [fname]M. N.[/fname][/pauthor], & [pauthor][surname]Zhu[/surname], [fname]B[/fname][/pauthor][/authors]. ([date dateiso="19990000" specyear="1999"]1999[/date]). [arttitle]Drying shrinkage of fibre-reinforced lightweight aggregate concrete containing fly ash[/arttitle]. [source]Cement and concrete research[/source], [volid]29[/volid]([issueno]11[/issueno]), [pages]1835-1840[/pages].[/ref]

[ref id="r25" reftype=“journal"][authors role="nd"][pauthor][surname]Kearsley[/surname], [fname]E. P.[/fname][/pauthor], [pauthor][surname]Wainwright[/surname], [fname]P. J.[/fname][/pauthor], & [pauthor][surname]Amtsbuchler[/surname], [fname]R[/fname][/pauthor][/authors]. ([date dateiso="20030000" specyear="2003"]2003[/date]). [arttitle]The effect of fly ash properties on concrete strength[/arttitle] In [source]Journal of the South African Institution of Civil Engineering[/source], [volid]45 [/volid]([issueno]1[/issueno]) 2003, pp. [pages]19-24[/pages]: [moreinfo]discussion. Journal of the South African Institution of Civil Engineering, Joernaal van die Suid-Afrikaanse Instituut van Siviele Ingenieurswese, 45(4), 18-19[/moreinfo].[/ref]

[ref id="r26" reftype=“journal"][authors role="nd"][pauthor][surname]Kearsley[/surname], [fname]Elsabé[/fname][/pauthor] & [pauthor][surname]Elsaigh[/surname], [fname]W[/fname][/pauthor][/authors]. ([date dateiso="20030000" specyear="2003"]2003[/date]). [arttitle]Effect of ductility on load-carrying capacity of steel fibre reinforced concrete ground slabs[/arttitle]. [source]Journal of the South African Institution of Civil Engineers[/source]. [volid]45[/volid]. [pages]25-30[/pages].[/ref]

[ref id="r27" reftype=“journal"][authors role="nd"][pauthor][surname]Kockal[/surname], [fname]N. U.[/fname][/pauthor], & [pauthor][surname]Ozturan[/surname], [fname]T[/fname][/pauthor][/authors]. ([date dateiso="20110000" specyear="2011"]2011[/date]). [arttitle]Durability of lightweight concretes with lightweight fly ash aggregates[/arttitle]. [source]Construction and Building Materials[/source], [volid]25[/volid]([issueno]3[/issueno]), [pages]1430-1438[/pages].[/ref]

[ref id="r28" reftype=“journal"][authors role="nd"][pauthor][surname]Kuang[/surname], [fname]J. S.[/fname][/pauthor], & [pauthor][surname]Morley[/surname], [fname]C. T[/fname][/pauthor][/authors]. ([date dateiso="19930000" specyear="1993"]1993[/date]). [arttitle]Punching shear behavior of restrained reinforced concrete slabs[/arttitle]. [source]Structural Journal[/source], [volid]89[/volid]([issueno]1[/issueno]), [pages]13-19[/pages].[/ref]

[ref id="r29" reftype=“journal"][authors role="nd"][pauthor][surname]Mahmoud[/surname], [fname]Z. I[/fname][/pauthor]., [pauthor][surname]El Tony[/surname], [fname]E[/fname][/pauthor]. [pauthor][surname]tony[/surname] [fname]M[/fname][/pauthor]., & [pauthor][surname]Saeed[/surname], [fname]K. S[/fname][/pauthor][/authors]. ([date dateiso="20180000" specyear="2018"]2018[/date]). [arttitle]Punching shear behavior of recycled aggregate reinforced concrete slabs[/arttitle]. [source]Alexandria Engineering Journal[/source], [volid]57[/volid]([issueno]2[/issueno]), [pages]841-849[/pages]. [/ref]

[ref id="r30" reftype=“journal"][authors role="nd"][pauthor][surname]Mohammadi[/surname], [fname]Y.[/fname][/pauthor], [pauthor][surname]Singh[/surname], [fname]S. P.[/fname][/pauthor], & [pauthor][surname]Kaushik[/surname], [fname]S. K[/fname][/pauthor][/authors]. ([date dateiso="20080000" specyear="2008"]2008[/date]). [arttitle]Properties of steel fibrous concrete containing mixed fibres in fresh and hardened state[/arttitle]. [source]Construction and Building Materials[/source], [volid]22[/volid]([issueno]5[/issueno]), [pages]956-965[/pages].[/ref]

[ref id="r31" reftype=“journal"][authors role="nd"][pauthor][surname]Nadesan[/surname], [fname]M. S.[/fname][/pauthor], & [pauthor][surname]Dinakar[/surname], [fname]P[/fname][/pauthor][/authors]. ([date dateiso="20170000" specyear="2017"]2017[/date]). [arttitle]Mix design and properties of fly ash waste lightweight aggregates in structural lightweight concrete[/arttitle]. [source]Case studies in construction materials[/source], [volid]7[/volid], [pages]336-347[/pages].[/ref]

[ref id="r32" reftype=“journal"][authors role="nd"][pauthor][surname]Nadesan[/surname], [fname]M. S.[/fname][/pauthor], & [pauthor][surname]Dinakar[/surname], [fname]P[/fname][/pauthor][/authors]. ([date dateiso="20170000" specyear="2017"]2017[/date]). [arttitle]Structural concrete using sintered fly ash lightweight aggregate: A review[/arttitle]. [source]Construction and Building Materials[/source], [volid]154[/volid], [pages]928-944[/pages].[/ref]

[ref id="r33" reftype=“journal"][authors role="nd"][pauthor][surname]Nemani[/surname], [fname]R. D. M.[/fname][/pauthor], [pauthor][surname]Rao[/surname], [fname]M. V. S.[/fname][/pauthor], & [pauthor][surname]Grandhe[/surname], [fname]V. V. S. N[/fname][/pauthor][/authors]. ([date dateiso="20160000" specyear="2016"]2016[/date]). [arttitle]Studies on Punching Shear Resistance of Two-Way Slab Specimens with Partial Replacement of Cement by GGBS with Different Edge Conditions[/arttitle]. [source]Journal of The Institution of Engineers[/source] ([publoc]India[/publoc]): Series A, [volid]97[/volid]([issueno]3[/issueno]), [pages]307-312[/pages].[/ref]

[ref id="r34" reftype=“journal"][authors role="nd"][pauthor][surname]Nguyen-Minh[/surname], [fname]L.[/fname][/pauthor], [pauthor][surname]Rovňák[/surname], [fname]M.[/fname][/pauthor], [pauthor][surname]Tran-Quoc[/surname], [fname]T.[/fname][/pauthor], & [pauthor][surname]Nguyenkim[/surname], [fname]K[/fname][/pauthor][/authors]. ([date dateiso="20110000" specyear="2011"]2011[/date]). [arttitle]Punching shear resistance of steel fiber reinforced concrete flat slabs[/arttitle]. [source]Procedia Engineering[/source], [volid]14[/volid], [pages]1830-1837[/pages].[/ref]

[ref id="r35" reftype=“journal"][authors role="nd"][pauthor][surname]Patra[/surname], [fname]S. N.[/fname][/pauthor], [pauthor][surname]Patra[/surname], [fname]R. K.[/fname][/pauthor], [pauthor][surname]Mukharjee[/surname], [fname]B. B.[/fname][/pauthor], & [pauthor][surname]Jena[/surname], [fname]S[/fname][/pauthor][/authors]. ([date dateiso="20210000" specyear="2021"]2021[/date]). [arttitle]Development of sustainable concrete incorporating metakaolin and sintered fly ash aggregate[/arttitle]. [source]Structural Concrete[/source].[/ref]

[ref id="r36" reftype=“journal"][authors role="nd"][pauthor][surname]Reis[/surname], [fname]N.[/fname][/pauthor], [pauthor][surname]de Brito[/surname], [fname]J.[/fname][/pauthor], [pauthor][surname]Correia[/surname], [fname]J. R.[/fname][/pauthor], & [pauthor][surname]Arruda[/surname], [fname]M. R[/fname][/pauthor][/authors]. ([date dateiso="20150000" specyear="2015"]2015[/date]). [arttitle]Punching behaviour of concrete slabs incorporating coarse recycled concrete aggregates[/arttitle]. [source]Engineering structures[/source], [volid]100[/volid], [pages]238-248[/pages].[/ref]

[ref id="r37" reftype=“journal"][authors role="nd"][pauthor][surname]Sermet[/surname], [fname]F.[/fname][/pauthor], & [pauthor][surname]Ozdemir[/surname], [fname]A[/fname][/pauthor][/authors]. ([date dateiso="20160000" specyear="2016"]2016[/date]). [arttitle]Investigation of punching behaviour of steel and polypropylene fibre reinforced concrete slabs under normal load[/arttitle]. [source]Procedia engineering[/source], [volid]161[/volid], [pages]458-465[/pages].[/ref]

[ref id="r38" reftype=“journal"][authors role="nd"][pauthor][surname]Shah[/surname], [fname]S. P.[/fname][/pauthor], [pauthor][surname]Daniel[/surname], [fname]J. I.[/fname][/pauthor], [pauthor][surname]Ahmad[/surname], [fname]S. H.[/fname][/pauthor], [pauthor][surname]Arockiasamy[/surname], [fname]M.[/fname][/pauthor], [pauthor][surname]Balaguru[/surname], [fname]P. N.[/fname][/pauthor], [pauthor][surname]Ball[/surname], [fname]C. G.[/fname][/pauthor], & [pauthor][surname]Zollo[/surname], [fname]R. F[/fname][/pauthor][/authors]. ([date dateiso="19930000" specyear="1993"]1993[/date]). [arttitle]Guide for specifying, proportioning, mixing, placing, and finishing steel fiber reinforced concrete[/arttitle]. [source]ACI Materials Journal[/source], [volid]90[/volid]([issueno]1[/issueno]), [pages]94-101[/pages].[/ref]

[ref id="r39" reftype=“journal"][authors role="nd"][pauthor][surname]Subramanian[/surname], [fname]N[/fname][/pauthor][/authors]. ([date dateiso="20050000" specyear="2005"]2005[/date]). [arttitle]Evaluation and enhancing the punching shear resistance of flat slabs using HSC[/arttitle]. [source]The Indian Concrete Journal[/source], [volid]79[/volid]([issueno]4[/issueno]), [pages]31-37[/pages].[/ref]

[ref id="r40" reftype=“journal"][authors role="nd"][pauthor][surname]Tuğrul Erdem[/surname], [fname]R[/fname][/pauthor][/authors]. ([date dateiso="20210000" specyear="2021"]2021[/date]). [arttitle]Dynamic responses of reinforced concrete slabs under sudden impact loading[/arttitle]. [source]Revista de la construcción[/source], [volid]20[/volid]([issueno]2[/issueno]), [pages]346-358[/pages].[/ref]

[ref id="r41" reftype=“journal"][authors role="nd"][pauthor][surname]Wainwright[/surname], [fname]P. J.[/fname][/pauthor], & [pauthor][surname]Robery[/surname], [fname]P[/fname][/pauthor][/authors]. ([date dateiso="19970000" specyear="1997"]1997[/date]). [arttitle]Structural performance of reinforced concrete made with sintered ash aggregate[/arttitle]. [source]Studies in environmental science[/source], [pages]411-419[/pages].[/ref]

[ref id="r42" reftype=“journal"][authors role="nd"][pauthor][surname]Youm[/surname], [fname]K. S.[/fname][/pauthor], [pauthor][surname]Kim[/surname], [fname]J. J.[/fname][/pauthor], & [pauthor][surname]Moon[/surname], [fname]J[/fname][/pauthor][/authors]. ([date dateiso="20140000" specyear="2014"]2014[/date]). [arttitle]Punching shear failure of slab with lightweight aggregate concrete (LWAC) and low reinforcement ratio[/arttitle]. [source]Construction and Building Materials[/source], [volid]65[/volid], [pages]92-102[/pages][/ref][/refs].

[/doc]